Test Results Fytocell® has been extensively tested for application in nursery stock. The results of which are without a doubt fantastic. Generally speaking, with the addition of Fytocell® to the potting soil an obvious improvement in the quality of the roots; number of branches and improvement in the complete plant system is achieved. The various tests are shown below.

| Sandy soil mixtures in plant holes | Improving the quality of cultivated soil | Improving the quality of potting soil | Establish the usage of Fytocell® in potting soil |
| --- | --- | --- | --- |
| Mixtures used: • Untreated • 15 volume % • 30 volume % | Mixtures used: • Untreated • 12,5 volume • 25 volume % | Mixtures used: • Untreated • 10 volume % • 20 volume % • 30 volume % | Mixtures used: • Lava floor, potting soil without Fytocell® • Lava floor, potting soil with 20 volume % Fytocell® • Concrete floor, potting soil without Fytocell® • Concrete floor, potting soil with 20 volume % Fytocell® |
| Measurements: | Measurements: | Measurements: | Measurements: |
| • Granular and chemical • Composition of the soil • Sagging calculation • Physical values • Sheer strength | • Granular and chemical • Composition of the soil • Sheer strength • Crop observation | • Physical potting soil research • Chemical analysis • Fertilization research • Crop observation | • Physical potting soil research • Chemical analysis • Fertilization research • Crop observation |
| Results: | Results: | Results: | Results: |
| • Increase in available nitrogen and potassium • Percentage fine particles rises • Record volume increase • All measured sagging values in the plant hole are low, when this is compared to the limit values of the condens-tion and rooting. | • Slight increase in availble nitrogen and potassium • Percentage organic matter increases • Plant length increases • Fresh and Dry weight of plants increased • Applying extra Fytocell results in an additional increase in length | • Air volume increased • Water volume increased • Greater number of branches • Better quality of the root • Healthier / more active roots | • Increase in air volume • Increase in water volume • Number of branches increased • Better root quality • Healthier / more active roots |

These test results can be sent to you free of charge on request.